AUTOFROTH® 104-B-9907 RESIN/ AUTOFROTH® 9300A ISOCYANATE

RIGID URETHANE FOAM SYSTEM

DESCRIPTION

Autofroth® 104-B-9907 Resin/ Autofroth® 9300A Isocyanate is a two-component polymeric MDI based system utilizing water and HFC134a as blowing agents.  This system is designed for insulation of discontinuous sandwich panels.

#### AUTOFROTH® 104-B-9907 RESIN COMPONENT

Appearance	Amber liquid

Odor	Slight Amine

Density, @77°F	10.6 lbs./gal.

Viscosity, @77°F	400 cps

Flash Point, ASTM 3278-89	>200°F

AUTOFROTH® 9300A ISOCYANATE COMPONENT

Appearance	Dark brown liquid

Odor	Slight aromatic

Density, @77°F	10.2 lbs./gal.

Viscosity, @77°F	200 cps

Flash Point	>400°F

Vapor Pressure, at 20°C	0.00016 mm Hg

TYPICAL PROCESSING PARAMETERS

Ratio by weight (A/B)	100/104 ± 5

Component Temperature, F	80

Mold Temperature, F 	100

Nominal Reactivity (sec.)

String Gel Time	110

Tack Time	150

Free Rise Density (pcf)	1.65

System developed on SL-360 equipment/standard mixer.   Foam characteristics will vary with different equipment.

AUTOFROTH® 104-B-9907 RESIN/ AUTOFROTH® 9300A ISOCYANATE

RIGID URETHANE FOAM SYSTEM

##### TYPICAL PHYSICAL PROPERTIES

Molded Panel, pcf	               	2.30

Core Density, pcf                                                          		2.10

Compressive Strength, psi @10% deflection

Parallel								20

Perpendicular							15

K-Factor, Initial (BTU-in/hr-ft2-ºF)			0.155

UL Subject 723 (File #R5692-6” Core Panels)/ASTM E-84):

Flame Spread1	25

Smoke Density	400

ASTM D-1929-91:

Minimum Self-Ignition Temperature			500C (932F)

Minimum Flash-Ignition Temperature			370C (698F)

Dimensional Stability, % Volume Change at 28 days

-20F	-2

100°F/100% RH	2

158°F	-1

158°F/100% RH	-1

200°F	0

1 This numerical flame spread rating is not intended to reflect hazards presented by this or any other material under actual fire conditions.

AUTOFROTH® 104-B-9907 RESIN/ AUTOFROTH® 9300A ISOCYANATE

RIGID URETHANE FOAM SYSTEM